## Slide 1
EU HARDWOODS
Progress report from UL FGG – Paris meeting
Goran Turk (UL FGG)
Mitja Plos (UL FGG)
Urška Bajc (UL FGG)

## Slide 2
LITERATURE SURVEY
The extensive literature of the dissertation from Ulrich Hübner has been checked for existing data on mechanical properties of hardwood species
Data from only 7 papers was taken (Aicher, Bachle, Blass, Frese, Fruhwald, Glos, Lanvin)
Further research will be done on other more recent publications
Additional testing will be done within the project on Slovenian beech

## Slide 3
GATHERED DATA
Species | Country | Density MOR | Bending MOR | Tension | MOE | MOEdyn
Beech | Germany | 84 |  |  |  | 84
Beech | Switzerland | 27 | 27 |  | 27 | 27
Beech | Germany | 27 | 27 |  | 27 | 27
Ash | Switzerland | 32 | 32 |  | 32 | 32
Beech | Germany | 1561 |  | 840 | 486 | 
Beech | Germany | 2151 |  |  |  | 
Beech | Germany |  |  | 69 |  | 
Beech | Germany |  |  | 219 |  | 
Oak | France | 420 | 420 |  | 420 | 

## Slide 4
FURTHER TESTING
Expand the data with visual, non-destructive and destructive data for single lamellas
Within the EU Hardwoods project tension tests will be done
Later bending tests on single lamellas and on glulam beams will also be done

## Slide 5
FURTHER TESTING - Material
Beech wood (Fagus sylvatica) from Slovenia
200 logs from sawmill GG Novo Mesto d.d.
Minimal length 3 m

## Slide 6
FURTHER TESTING - Sample
4 pieces from each log = 800 pieces
Dimensions: 48 mm x 150 mm
200 pieces for tension tests on single lamellas (EU Hardwood)
200 pieces for bending tests on single lamellas
400 pieces for the production of glulam beams

## Slide 7
FURTHER TESTING - Glulam
40 glulam beams – 5 lamellas per height
Glulam beams dimensions: 150 mm x 240 mm x 5000 mm
Glulam beams production at glulam company HOJA d.d.

## Slide 8
FURTHER TESTING – NDT + Destructive tests
Visual grading (DIN 4074-5, KAR, BS 5756)
Longitudinal Eigen frequency
Transverse Eigen frequency
Speed of ultrasound
Destructive testing

## Slide 9
DISSEMINATION
Project logo
LinkedIN project page
Updated web page
Presentation of the project at a small WoodWisdom-NET+ conference in Slovenia (second year round)
FVA will present a paper at the International Scientific Conference on Hardwood Processing in Quebec City

## Slide 10
eu-hardwoods.eu
goran.turk@fgg.uni-lj.si
mitja.plos@fgg.uni-lj.si
urska.bajc@fgg.uni-lj.si